- Drainage-channel BG-FILCOTEN light mini NW 150 made of FILCOTEN HPC (high-performance concrete)

load-class A15 – C250 kN, according to EN1433 – CE-certified,

channel joint with safety seam, sealable,

length 1000 mm, without slope

Building biology tested and recommended by IBR (Institut für Baubiologie Rosenheim, DE)

Fire-behaviour class: A1 according to EN13501 - non-combustible

100% recyclable with U-A marking

Delivery and installation according to the manufacturer's installation instructions.

NW/No.:		LxWxH: [mm]		weight: [kg]	eco-indicator: [kg]

150 BH 100:		1000x180x100		16,8		CO2-Eq. 4,7

- Surcharge for bottom outlet DN 150

- Covers/Grates made of galvanised steel, stainless steel 1.4301 or cast iron, with clamping device,

load class A15kN – C250kN, according to EN1433 – CE-certified

BG-FILCOTEN light mesh grating NW 150, galvanised steel or stainless steel

cl. B125, MW 30/10, length 1000 mm, according to EN1433 - CE-certified

BG-FILCOTEN light mesh grating NW 150, galvanised steel or stainless steel

cl. B125, MW 30/10, length 500 mm, according to EN1433 - CE-certified

Patent clamp for mesh grating, galvanised steel

BG-FILCOTEN light slotted grating NW 150, galvanised steel or stainless steel

cl. A15, SW 8/80, length 1000 mm, according to EN1433 - CE-certified

BG-FILCOTEN light slotted grating NW 150, galvanised steel or stainless steel

cl. A15, SW 8/80, length 500 mm, according to EN1433 - CE-certified

BG-FILCOTEN light ductile-iron mesh grating NW 150, ductile-iron EN-GJS

cl. C250, MW 15/25, length 500 mm, according to EN1433 - CE-certified

Patent clamp for ductile-iron mesh grating, steel black painted

Holding clamp for ductile iron mesh grating, steel black painted

- Slot top asymmetric made of galvanised steel or stainless steel 1.4301, SW 12,5mm

or slot top 2S, SW 2x6mm or 3S, SW 3x6mm, load class: C250; SH 110mm

BG-FILCOTEN light/tec slot top asymmetric, NW 150, galvanised steel or stainless steel

cl. C250, SW 12,5 mm, length 1000 mm, SH 110mm

BG-FILCOTEN light/tec slot top asymmetric, NW 150, galvanised steel or stainless steel

cl. C250, SW 12,5 mm, length 500 mm, SH 110mm

BG-FILCOTEN light/tec slot top maintenance unit asymmetric, NW 150, galvanised steel or stainless steel

cl. C250, SW 12,5 mm, length 500 mm, SH 110mm

BG-FILCOTEN light/tec slot top 2S asymmetric, NW 150, galvanised steel or stainless steel

cl. C250, SW 2x6 mm, length 1000 mm, SH 110mm

BG-FILCOTEN light/tec slot top 2S asymmetric, NW 150, galvanised steel or stainless steel

cl. C250, SW 2x6 mm, length 500 mm, SH 110mm

BG-FILCOTEN light/tec slot top 2S maintenance unit asymmetric, NW 150, galvanised steel or stainless steel

cl. C250, SW 2x6 mm, length 500 mm, SH 80mm

BG-FILCOTEN light/tec slot top 3S asymmetric, NW 150, stainless steel

cl. C250, SW 3x6 mm, length 1000 mm, SH 110mm

BG-FILCOTEN light/tec slot top 3S asymmetric, NW 150, stainless steel

cl. C250, SW 3x6 mm, length 500 mm, SH 110mm

BG-FILCOTEN light/tec slot top 3S maintenance unit asymmetric, NW 150, stainless steel

cl. C250, SW 3x6 mm, length 500 mm, SH 110mm

Construction time barrier for slot top SW 12,5mm and SW 2x6 mm, L = 1000 mm, wood

BG-cover tape, for slot tops, white, width 50mm, 33m/roll

Opening tool for maintenance unit cover – 2 pcs. required, galvanised steel/plastic

- sump unit kit BG-FILCOTEN light NW 100 made of FILCOTEN HPC (high-performance concrete)

incl. silt bucket

outlet: pipe coupling DN 150

lenght 500 mm / width 195 mm / height 650 mm

Delivery and installation according to the manufacturer's installation instructions.

weight: 45,3 kg

Odour trap for retrofitting for sump unit, plastic

weight: 0,2 kg

- front cap closed, made of galvanised steel or stainless steel 1.4301

weight: 0,5 kg

- installation chair, Kit incl. screws for positioning the channel, galvanised steel weight: 1,7 kg