- Drainage-channel BG-FILCOTEN pro NW 100 made of FILCOTEN HPC (high-performance concrete)

with integrated edge made of galvanised steel, stainless steel 1.4301 or cast iron,

load-class A15 – E600 kN, according to EN1433 – CE-certified,

channel joint with safety seam, sealable,

length 1000 mm, without or with 0,5 % slope

Building biology tested and recommended by IBR (Institut für Baubiologie Rosenheim, DE)

Fire-behaviour class: A1 according to EN13501 - non-combustible

100% recyclable with U-A marking

Delivery and installation according to the manufacturer's installation instructions.

NW/No.:		LxWxH: [mm]		weight: [kg]	eco-indicator: [kg]

Galvanised steel edge:

100 No. 0:		1000x138x142		18,3		CO2-Eq. 8,9

100 No. 20-0:		1000x138x245		31,0		CO2-Eq. 12,4

100 No. 1-10:		1000x138x145-195	18,6-24,6	CO2-Eq.  9,0 – 11,9

Cast iron edge:

100 No. 0:		1000x138x142		19,1		CO2-Eq. 11,5

100 No. 20-0:		1000x138x245		32,0		CO2-Eq. 15,1

100 No. 1-10:		1000x138x145-195	19,5-25,4	CO2-Eq.  11,7 – 15,3

Stainless steel edge:

100 No. 0:		1000x138x142		18,3		CO2-Eq. 6,8

100 No. 20-0:		1000x138x245		31,0		CO2-Eq. 10,4

100 No. 1-10:		1000x138x145-195	18,6-24,6	CO2-Eq.  6,9 – 9,1

- Drainage-channel as described in position 1, but

overall length 500 mm, without slope

NW/No.:		LxWxH: [mm]		weight: [kg]	eco-indicator: [kg]

Galvanized steel edge:

100 No. 0:		500x138x142		 9,6		CO2-Eq. ca. 4,8

100 No. 5-0:		500x138x170		13,2		CO2-Eq. ca. 6,5 	(plain sidewall)

100 No. 10-0:		500x138x195		12,5		CO2-Eq. ca. 6,1

Cast iron edge:

100 No. 0:		500x138x142		 9,7		CO2-Eq. ca. 5,9

100 No. 5-0:		500x138x170		13,5		CO2-Eq. ca. 8,2 	(plain sidewall)

100 No. 10-0:		500x138x195		13,1		CO2-Eq. ca. 7,9

Stainless steel edge:

100 No. 0:		500x138x142		 9,6		CO2-Eq. ca. 3,6

100 No. 5-0:		500x138x170		13,2		CO2-Eq. ca. 5,0 	(plain sidewall)

100 No. 10-0:		500x138x195		12,5		CO2-Eq. ca. 4,7

- Surcharge for bottom outlet DN 100,

for drainage channels without slope

- Covers/Grates made of galvanised steel, stainless steel 1.4301, ductile iron or plastic with integrated longitudinal movement protection and fiX-lock or 4-fold screw connection, load class A 15kN – E 600kN, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro mesh grating NW 100, galvanised steel or stainless steel

cl. C250, MW 30/10, length 1000 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro mesh grating NW 100, galvanised steel or stainless steel

cl. C250, MW 30/10, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro mesh grating NW 100, galvanised steel or stainless steel

cl. D400, MW 25/10, length 1000 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro mesh grating NW 100, galvanised steel or stainless steel

cl. D400, MW 25/10, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro slotted grating NW 100, galvanised steel or stainless steel

cl. C250, SW 8/80, length 1000 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro slotted grating NW 100, galvanised steel or stainless steel

cl. C250, SW 8/80, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro perforated grating NW 100, galvanised steel or stainless steel

cl. C250, DM 6, length 1000 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro perforated grating NW 100, galvanised steel or stainless steel

cl. C250, DM 6, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro COMBee-designgrate NW 100, plastic PA6

cl. B125, DM 7,3; length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro COMBee-designgrate NW 100, plastic PA6

cl. C250, DM 7,3; length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro ductile-iron bar grating NW 100, ductile-iron EN-GJS

cl. C250, MW 29/13, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro ductile-iron bar grating NW 100, ductile-iron EN-GJS

cl. C250, MW 29/6, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron bar grating NW 100, ductile-iron EN-GJS

cl. D400, MW 29/13, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron bar grating NW 100, ductile-iron EN-GJS

cl. D400, MW 28/9, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron slotted grating NW 100, ductile-iron EN-GJS

cl. E600, SW 14/100, length 500 mm

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron design-grate „VIA“ NW 100, ductile-iron EN-GJS

cl. D400, SW 7, length 500 mm

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron design-grate „KIARO“ NW 100, ductile-iron EN-GJS

cl. D400, SW 7, length 500 mm

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron design-grate „VILLE“ NW 100, ductile-iron EN-GJS

cl. E600, SW 7, length 500 mm

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

Anti-vandalism locking device made of stainless steel

cross piece for blocking the fiX-lock

BG-FILCOTEN pro ductile-iron bar grating NW 100, ductile-iron EN-GJS

cl. E600, MW 22/13, length 500 mm

with integrated longitudinal movement protection, 4-fold screw-connection (only in cast-iron edge), according to EN1433 - CE-certified, bolting material must be ordered separately, bolting material is exchangeable.

KIT-bolting material for ductile iron grating

steel, black galvanised - consisting of 1 pc. screw and 1 pc. nut (requirement: 8 pcs./m)

KIT-bolting material for ductile iron grating

stainless steel A2 - consisting of 1 pc. screw and 1 pc. nut (requirement: 8 pcs./m)

- sump unit kit BG-FILCOTEN pro NW 100 made of FILCOTEN HPC (high-performance concrete)

with integrated edge made of galvanised steel, stainless steel 1.4301 or cast iron, incl. silt bucket

outlet: pipe coupling DN 100

length 500 mm / width 145 mm / height 600 mm

Delivery and installation according to the manufacturer's installation instructions.

Galvanised steel edge:	32.6 kg

Cast iron edge: 	33.1 kg

Stainless steel edge: 	32.6 kg

Odour trap for retrofitting for sump unit, plastic

weight: 0,2 kg

- front-/end cap, outlet DN100, made of plastic, PP

weight: 0,1 kg

- installation chair, Kit incl. screws for positioning the channel, galvanised steel

weight: 1,5 kg

- odour trap for bottom outlet DN 100, plastic

weight: 0,2 kg