- Drainage-channel BG-FILCOTEN pro NW 150 made of FILCOTEN HPC (high-performance concrete)

with integrated edge out of galvanised steel, stainless steel 1.4301 or cast iron,

load-class A15 – E600 kN, according to EN1433 – CE-certified,

channel joint with safety seam, sealable,

length 1000 mm, without or with 0,5 % slope

Building biology tested and recommended by IBR (Institut für Baubiologie Rosenheim, DE)

Fire-behaviour class: A1 according to EN13501 - non-combustible

100% recyclable with U-A marking

Delivery and installation according to the manufacturer's installation instructions.

NW/No.:		LxWxH: [mm]		weight: [kg]	eco-indicator: [kg]

Galvanised steel edge:

150 No. 0:		1000x188x210		31,0		CO2-Eq. 12,4

150 No. 20-0:		1000x188x310		47,7		CO2-Eq. 17,0

150 No. 1-10:		1000x188x210-260	31,5-37,5	CO2-Eq. 12,6-15,0

Cast iron edge:

150 No. 0:		1000x188x210		31,8		CO2-Eq. 15,0

150 No. 20-0:		1000x188x310		48,7		CO2-Eq. 19,7

150 No. 1-10:		1000x188x210-260	32,5-38,5	CO2-Eq. 15,3-18,2

Stainless steel edge:

150 No. 0:		1000x188x210		31,0		CO2-Eq. 10,4

150 No. 20-0:		1000x188x310		47,7		CO2-Eq. 15,0

150 No. 1-10:		1000x188x210-260	31,5-37,5	CO2-Eq. 10,6-12,6

- Drainage-channel as described in position 1, but

overall length 500 mm, without slope

NW/No.:		LxBxH: [mm]		Gewicht: [kg]	Umweltkennzahl: [kg]

Galvanised steel edge:

150 No. 0:		500x188x210		15,2		CO2-Eq. ca. 6,1

150 No. 5-0:		500x188x235		20,7		CO2-Eq. ca. 8,3 	(plain sidewall)

150 No. 10-0:		500x188x260		19,3		CO2-Eq. ca. 7,8

Cast iron edge:

150 No. 0:		500x188x210		15,7		CO2-Eq. ca. 7,5

150 No. 5-0:		500x188x235		21,2		CO2-Eq. ca. 10,1 	(plain sidewall)

150 No. 10-0:		500x188x260		19,8		CO2-Eq. ca. 9,4

Stainless steel edge:

150 No. 0:		500x188x210		15,2		CO2-Eq. ca. 5,2

150 No. 5-0:		500x188x235		20,7		CO2-Eq. ca. 7,0	(plain sidewall)

150 No. 10-0:		500x188x260		19,3		CO2-Eq. ca. 6,5

- Surcharge for bottom outlet DN 150,

for drainage channels without slope

- Covers/Grates made of galvanised steel, stainless steel 1.4301 or cast iron with integrated longitudinal movement protection and fiX-lock or 4-fold screw connection, load class A 15kN – E 600kN, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro mesh grating NW 150, galvanised steel or stainless steel

cl. C250, MW 30/10, length 1000 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro mesh grating NW 150, galvanised steel or stainless steel

cl. C250, MW 30/10, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro mesh grating NW 150, galvanised steel or stainless steel

cl. D400, MW 25/10, length 1000 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro mesh grating NW 150, galvanised steel or stainless steel

cl. D400, MW 25/10, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro perforated grating NW 150, galvanised steel or stainless steel

cl. C250, DM 6, length 1000 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro perforated grating NW 150, galvanised steel or stainless steel

cl. C250, DM 6, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro ductile-iron bar grating NW 150, ductile-iron EN-GJS

cl. C250, MW 29/13, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron bar grating NW 150, ductile-iron EN-GJS

cl. D400, MW 29/13, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron bar grating NW 150, ductile-iron EN-GJS

cl. D400, MW 28/9, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron slotted grating NW 150, ductile-iron EN-GJS

cl. E600, SW 14/150, length 500 mm

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron design-grate „VIA“ NW 150, ductile-iron EN-GJS

cl. D400, SW 7, length 500 mm

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron design-grate „KIARO“ NW 150, ductile-iron EN-GJS

cl. D400, SW 7, length 500 mm

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron design-grate „VILLE“ NW 150, ductile-iron EN-GJS

cl. E600, SW 7, length 500 mm

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

Anti-vandalism locking device made of stainless steel

cross piece for blocking the fiX-lock

BG-FILCOTEN pro ductile-iron slotted grating NW 150, ductile-iron EN-GJS

cl. D400, SW 14/150, length 500 mm

with integrated longitudinal movement protection, 4-fold screw-connection (only in cast-iron edge), according to EN1433 - CE-certified, bolting material must be ordered separately, bolting material is exchangeable.

BG-FILCOTEN pro ductile-iron bar grating NW 150, ductile-iron EN-GJS

cl. E600, MW 22/13, length 500 mm

with integrated longitudinal movement protection, 4-fold screw-connection (only in cast-iron edge), according to EN1433 - CE-certified, bolting material must be ordered separately, bolting material is exchangeable.

KIT-bolting material for ductile iron grating

steel, black galvanised - consisting of 1 pc. screw and 1 pc. nut (requirement: 8 pcs./m)

KIT-bolting material material for ductile iron grating

stainless steel A2 - consisting of 1 pc. screw and 1 pc. nut (requirement: 8 pcs./m)

- sump unit kit BG-FILCOTEN pro NW 100 made of FILCOTEN HPC (high-performance concrete)

with integrated edge made of galvanised steel, stainless steel 1.4301 or cast iron, incl. silt bucket

outlet: pipe coupling DN 150

length 500 mm / width 200 mm / height 690 mm

Delivery and installation according to the manufacturer's installation instructions.

Galvanised steel frame: 44,8 kg

Cast iron frame:	 45,3 kg

Stainless steel frame: 	 44,8 kg

Odour trap for retrofitting for sump unit, plastic

weight: 0,2 kg

- front cap closed, out of galvanised steel or stainless steel 1.4301

weight: 0,5 kg

- end cap, with outlet DN150 out of galvanised steel or stainless steel 1.4301

weight: 0,6 kg

- Installation chair, Kit incl. screws for positioning the channel, galvanised steel

weight: 1,7 kg