- Drainage-channel BG-FILCOTEN pro NW 300 made of FILCOTEN HPC (high-performance concrete)

with integrated edge made of galvanised steel or cast iron,

load-class A15 – E600 kN, according to EN1433 – CE-certified,

channel joint with safety seam, sealable,

length 1000 mm, without or with 0,5 % slope

Building biology tested and recommended by IBR (Institut für Baubiologie Rosenheim, DE)

Fire-behaviour class: A1 according to EN13501 - non-combustible

100% recyclable with U-A marking

Delivery and installation according to the manufacturer's installation instructions.

NW/No.:		LxWxH: [mm]		weight: [kg]	eco-indicator: [kg]

Galvanised steel edge:

300 No. 0:		1000x360x360		75,6		CO2-Eq. 26,2

300 No. 20-0:		1000x360x460		109,0		CO2-Eq. 35,5

300 No. 1-10:		1000x360x360-410	76,3-88,0	CO2-Eq. 26,5-30,5

Cast iron edge:

300 No. 0:		1000x360x360		77,3		CO2-Eq. 30,7

300 No. 20-0:		1000x360x460		110,7		CO2-Eq. 40,0

300 No. 1-10:		1000x360x360-410	78,0-89,7	CO2-Eq. 31,0-35,6

- Drainage-channel as described in position 1, but

overall length 500 mm, without slope

NW/No.:		LxWxH: [mm]		weight: [kg]	eco-indicator: [kg]

Galvanized steel edge:

300 No. 0:		500x360x360		37,9		CO2-Eq. ca. 13,2

Cast iron edge:

300 No. 0:		500x360x360		38,8		CO2-Eq. ca. 15,4

- Surcharge for bottom outlet DN 200,

for drainage channels without slope

- Covers/Grates made of galvanised steel, stainless steel 1.4301 or cast iron with integrated longitudinal movement protection and fiX-lock or 4-fold screw connection, load class A 15kN – E 600kN, according to EN1433 - CE-certified

BG-FILCOTEN pro mesh grating NW 300, galvanised steel or stainless steel

cl. C250, MW 30/10, length 1000 mm,

with integrated longitudinal movement protection, 4-fold screw connection, according to EN1433 - CE-certified

BG-FILCOTEN pro mesh grating NW 300, galvanised steel or stainless steel

cl. C250, MW 30/10, length 500 mm,

with integrated longitudinal movement protection, 4-fold screw connection, according to EN1433 - CE-certified

KIT-bolting material for mesh grating

galvanised steel - consisting of 1 pc. screw and 1 pc. nut (requirement: 4 pcs./m)

BG-FILCOTEN pro ductile-iron bar grating NW 300, ductile-iron EN-GJS

cl. D400, MW 29/13, length 500 mm,

with integrated longitudinal movement protection, 4-fold screw connection, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron bar grating NW 300, ductile-iron EN-GJS

cl. E600, MW 29/13, length 500 mm,

with integrated longitudinal movement protection, 4-fold screw connection, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron slotted grating NW 300, ductile-iron EN-GJS

cl. D400, SW 16/300, length 500 mm

with integrated longitudinal movement protection, 4-fold screw connection, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron design-grate “VIA“ NW 300, ductile-iron EN-GJS

cl. D400, SW 6, length 500 mm

with integrated longitudinal movement protection, 4-fold screw connection, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron design-grate “KIARO“ NW 300, ductile-iron EN-GJS

cl. D400, SW 7, length 500 mm

with integrated longitudinal movement protection, 4-fold screw connection, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron design-grate “VILLE“ NW 300, ductile-iron EN-GJS

cl. E600, SW 8, length 500 mm

with integrated longitudinal movement protection, 4-fold screw connection, according to EN1433 - CE-certified

KIT-bolting material for ductile iron grating cl. D400 – E600

steel, black galvanised - consisting of 1 pc. screw and 1 pc. nut (requirement: 8 pcs./m)

KIT-bolting material for ductile iron grating cl. D400 – E600

stainless steel A2 - consisting of 1 pc. screw and 1 pc. nut (requirement: 8 pcs./m)

- sump unit kit BG-FILCOTEN pro NW 300 made of FILCOTEN HPC (high-performance concrete)

with integrated edge made of galvanised steel, stainless steel 1.4301 or cast iron, incl. silt bucket

outlet: pipe coupling DN 200

length 560 mm / width 520 mm / height 950 mm

Delivery and installation according to the manufacturer's installation instructions.

Galvanised steel edge:	126,2 kg

Cast iron edge:	127,2 kg

- front cap closed, made of galvanised steel or stainless steel 1.4301

weight: 1,7 kg

- end cap, with outlet DN200 made of galvanised steel

weight: 1,6 kg

- installation chair, Kit incl. screws for positioning the channel, galvanised steel

weight: 2,1 kg