- Drainage-channel BG-FILCOTEN pro mini NW 100 made of FILCOTEN HPC (high-performance concrete)

with integrated edge made of galvanised steel, stainless steel 1.4301 or cast iron,

load-class A15 – E600 kN, according to EN1433 – CE-certified,

channel joint with safety seam, sealable,

length 1000 mm, without slope

Building biology tested and recommended by IBR (Institut für Baubiologie Rosenheim, DE)

Fire-behaviour class: A1 according to EN13501 - non-combustible

100% recyclable with U-A marking

Delivery and installation according to the manufacturer's installation instructions.

NW/No.:		LxWxH: [mm]		weight: [kg]	eco-indicator: [kg]

Galvanised steel edge:

100 BH 60:		1000x138x60		9,1		CO2-Eq. 6,3

100 BH 80:		1000x138x80		10,7		CO2-Eq. 6,8

Cast iron edge:

100 BH 80:		1000x138x80		11,1		CO2-Eq. 9,3

Stainless steel edge:

100 BH 60:		1000x138x60		9,1		CO2-Eq. 4,3

100 BH 80:		1000x138x80		10,7		CO2-Eq. 4,7

- Surcharge for bottom outlet DN100

- Covers/Grates made of galvanised steel, stainless steel 1.4301, cast iron or plastic with integrated longitudinal movement protection and fiX-lock or 4-fold screw connection, load class A 15kN – E 600kN, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro mesh grating NW 100, galvanised steel or stainless steel

cl. C250, MW 30/10, length 1000 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro mesh grating NW 100, galvanised steel or stainless steel

cl. C250, MW 30/10, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro mesh grating NW 100, galvanised steel or stainless steel

cl. D400, MW 25/10, length 1000 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro mesh grating NW 100, galvanised steel or stainless steel

cl. D400, MW 25/10, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro slotted grating NW 100, galvanised steel or stainless steel

cl. C250, SW 8/80, length 1000 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro slotted grating NW 100, galvanised steel or stainless steel

cl. C250, SW 8/80, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro perforated grating NW 100, galvanised steel or stainless steel

cl. C250, DM 6, length 1000 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro perforated grating NW 100, galvanised steel or stainless steel

cl. C250, DM 6, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro COMBee-design grate NW 100, plastic PA6

cl. B125, DM 7,3; length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro COMBee-designgrate NW 100, plastic PA6

cl. C250, DM 7,3; length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro ductile-iron bar grating NW 100, ductile-iron EN-GJS

cl. C250, MW 29/13, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN tec/pro ductile-iron bar grating NW 100, ductile-iron EN-GJS

cl. C250, MW 29/6, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron bar grating NW 100, ductile-iron EN-GJS

cl. D400, MW 29/13, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron bar grating NW 100, ductile-iron EN-GJS

cl. D400, MW 28/9, length 500 mm,

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron slotted grating NW 100, ductile-iron EN-GJS

cl. E600, SW 14/100, length 500 mm

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron design-grate “VIA“ NW 100, ductile-iron EN-GJS

cl. D400, SW 7, length 500 mm

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron design-grate “KIARO“ NW 100, ductile-iron EN-GJS

cl. D400, SW 7, length 500 mm

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

BG-FILCOTEN pro ductile-iron design-grate “VILLE“ NW 100, ductile-iron EN-GJS

cl. E600, SW 7, length 500 mm

with integrated longitudinal movement protection and fiX-lock, according to EN1433 - CE-certified

Anti-vandalism locking device made of stainless steel

cross piece for blocking the fiX-lock

BG-FILCOTEN pro ductile-iron bar grating NW 100, ductile-iron EN-GJS

cl. E600, MW 22/13, length 500 mm

with integrated longitudinal movement protection, 4-fold screw-connection (only in cast-iron edge), according to EN1433 - CE-certified, bolting material must be ordered separately, bolting material is exchangeable.

KIT-bolting material for ductile iron grating

steel, black galvanised - consisting of 1 pc. screw and 1 pc. nut (requirement: 8 pcs./m)

KIT-bolting material for ductile iron grating

stainless steel A2 - consisting of 1 pc. screw and 1 pc. nut (requirement: 8 pcs./m)

- sump unit kit BG-FILCOTEN pro NW 100 made of FILCOTEN HPC (high-performance concrete)

with integrated edge made of galvanised steel, stainless steel 1.4301 or cast iron, incl. silt bucket

outlet: pipe coupling DN 100

length 500 mm / width 145 mm / height 600 mm

Delivery and installation according to the manufacturer's installation instructions.

Galvanised steel edge:	32.6 kg

Cast iron edge:	33.1 kg

Stainless steel edge: 	32.6 kg

Odour trap for retrofitting for sump unit, plastic

weight: 0,1 kg

- front cap closed, made of galvanised steel or stainless steel 1.4301

weight: 0,1 kg

- installation chair, Kit incl. screws for positioning the channel, galvanised steel

weight: 1,5 kg

- odour trap for bottom outlet DN 100, plastic

weight: 0,2 kg