- Monolithic drainage channel BG-FILCOTEN one NW 150 made of FILCOTEN HPC (High Performance Concrete)

Load class F900 kN - Type M resp. D400 – Type I, tested according to EN1433; CE-certified

Channel element with integrated anchorage pockets, channel joint sealable

Double inlet-slots radially counter-rotating, 23/52 mm, according to EN 1433

Inlet cross section min. 370 cm²/m

Channel cross section in W-shape, optimized for partial / complete filling

Building biology tested and recommended by IBR (Institut für Baubiologie Rosenheim, DE)

Fire-behaviour class: A1 according to EN13501 - non-combustible

100% recyclable with U-A marking

Delivery and installation according to the manufacturer's installation instructions.

NW/No.:		LxWxH: [mm]	weight: [kg]	discharge cross-section: [cm²]	eco-indicator: [kg]

NW150-0:		1000x210x300	76,6		220				CO2-Eq. 21,3

NW150 40-0:		1000x210x500	107,5		520				CO2-Eq. 29,8

- Revision-element No. 0 / 40-0, channel-element as described in position 1, but

with integrated edge out of cast iron and 4-fold screw connected ductile iron grate in cl. F900,

for cleaning and maintaining of the channel run

NW/No.:		LxWxH: [mm]	weight: [kg]	discharge cross-section: [cm²]	eco-indicator: [kg]

NW150-0:		1000x210x300	83,0		220				CO2-Eq. 40,0

NW150 40-0:		1000x210x500	111,0		520				CO2-Eq. 47,8

- Corner-element variable No. 0 / 40-0, channel-element as described in position 1, but

with partly closed surface, mitre-cut and bonded together,

angles from 90-180° are possible in the line.

- Outlet unit No. 0 / 40-0, revision-element as described in position 2, but

with outlet-drilling DN 150

NW/No.:		LxWxH: [mm]	weight: [kg]	discharge cross-section: [cm²]	eco-indicator: [kg] NW150-0:		1000x210x300	82,0		220				CO2-Eq. -

NW150 40-0:		1000x210x500	110,0		520				CO2-Eq. -

- Sump-unit upper part No. 0 / 40-0, revision-element as described in position 2, but

with outlet opening, on top of the outlet-unit lower-part and/or sump unit middle part

NW/No.:		LxWxH: [mm]	weight: [kg]	discharge cross-section: [cm²]	eco-indicator: [kg] NW150-0:		1000x210x300	79,0		220				CO2-Eq. 38,9

NW150 40-0:		1000x210x500	108,0		520	 			CO2-Eq. 47,0

- Sump-unit middle-part, made of FILCOTEN HPC

Measurements: 	LxWxH: 500x240x300 mm	weight: 28,0 kg

- Sump-unit lower-part with pipe-coupling DN150, made of FILCOTEN HPC

Measurements: 	LxWxH: 500x245x480 mm	weight: 33,8 kg		outlet: pipe-coupling DN 150

- Sump-unit lower-part with pipe-coupling DN200, made of FILCOTEN HPC

Measurements: 	LxWxH: 500x245x480 mm	weight: 33,3 kg		outlet: pipe-coupling DN 200

- Silt bucket made of plastic, weight 0,4 kg

- Front-plate No. 0 / 40-0, made of FILCOTEN HPC

NW150-0:		LxWxH: 54x210x300 mm		weight: 7 kg

NW150 40-0:		LxWxH: 54x210x500 mm		weight: 12 kg

- End-plate with outlet DN150, No. 0 / 40-0, made of FILCOTEN HPC

NW150-0:		LxWxH: 54x210x300 mm		weight: 5 kg

NW150 40-0:		LxWxH: 54x210x500 mm		weight: 10 kg

- Connector-plate for stepped-fall No. 0 to 40-0, made of FILCOTEN HPC

NW150 0/40-0:	LxWxH: 73x210x500 mm		weight: 9 kg

- Lifting hook kit, consisting of 2 pcs., made of steel, painted green, weight: 1.9 kg

- Sealing profile, pluggable or commercial sealing material on PU-basis