- Monolithic drainage channel BG-FILCOTEN one NW 200 made of FILCOTEN HPC (High Performance Concrete)

Load class F900 kN - Type M resp. D400 – Type I, tested according to EN1433; CE-certified

Channel element with integrated anchorage pockets, channel joint sealable

Double inlet-slots radially counter-rotating, 23/70 mm, according to EN 1433

Inlet cross section min. 510 cm²/m

Channel cross section in W-shape, optimized for partial / complete filling

Building biology tested and recommended by IBR (Institut für Baubiologie Rosenheim, DE)

Fire-behaviour class: A1 according to EN13501 - non-combustible

100% recyclable with U-A marking

Delivery and installation according to the manufacturer's installation instructions.

NW/No.:		LxWxH: [mm]	weight: [kg]	discharge cross-section: [cm²]	eco-indicator: [kg]

NW200-0:		1000x260x335	99,0		340				CO2-Eq. 27,5

NW200 40-0:		1000x260x535	131,5		735				CO2-Eq. 36,5

- Revision-element No. 0 / 40-0, channel-element as described in position 1, but

with integrated edge out of cast iron and 4-fold screw connected ductile iron grate in cl. F900,

for cleaning and maintaining of the channel run

NW/No.:		LxWxH: [mm]	weight: [kg]	discharge cross-section: [cm²]	eco-indicator: [kg]

NW200-0:		1000x260x335	101,0		340				CO2-Eq. 48,1

NW200 40-0:		1000x260x535	133,0		735				CO2-Eq. 57,0

- Corner-element variable No. 0 / 40-0, channel-element as described in position 1, but

with partly closed surface, mitre-cut and bonded together,

angles from 90-180° are possible in the line.

- Outlet unit No. 0 / 40-0, revision-element as described in position 2, but

with outlet-drilling DN 200

NW/No.:		LxWxH: [mm]	weight: [kg]	discharge cross-section: [cm²]	eco-indicator: [kg] NW200-0:		1000x260x335	99,0		340				CO2-Eq. -

NW200 40-0:		1000x260x535	131,0		735				CO2-Eq. -

- Sump-unit upper part No. 0 / 40-0, revision-element as described in position 2, but

with outlet opening, on top of the outlet-unit lower-part and/or sump unit middle part

NW/No.:		LxWxH: [mm]	weight: [kg]	discharge cross-section: [cm²]	eco-indicator: [kg] NW200-0:		1000x260x335	96,0		340				CO2-Eq. 46,7

NW200 40-0:		1000x260x535	128,0		735				CO2-Eq. 55,6

- Sump-unit middle-part, made of FILCOTEN HPC

Measurements: 	LxWxH: 500x290x300 mm	weight: 29,0 kg

- Sump-unit lower-part with pipe-coupling DN200, made of FILCOTEN HPC

Measurements: 	LxWxH: 500x309x480 mm	weight: 35,5 kg		outlet: pipe-coupling DN 200

- Sump-unit lower-part with pipe-coupling DN300, made of FILCOTEN HPC

Measurements: 	LxWxH: 500x332x480 mm	weight: 39,0 kg		outlet: pipe-coupling DN 300

- Silt bucket made of plastic, weight 0,7 kg

- Front-plate No. 0 / 40-0, made of FILCOTEN HPC

NW200-0:		LxWxH: 69x265x335 mm		weight: 13,0 kg

NW200 40-0:		LxWxH: 69x265x535 mm		weight: 21,0 kg

- End-plate with outlet DN150, No. 0 / 40-0, made of FILCOTEN HPC

NW200-0:		LxWxH: 69x265x335 mm		weight: 8,5 kg

NW200 40-0:		LxWxH: 69x265x535 mm		weight: 16,5 kg

- Connector-plate for stepped-fall No. 0 to 40-0, made of FILCOTEN HPC

NW200 0/40-0:	LxWxH: 73x260x535 mm		weight: 12,5 kg

- Lifting hook kit, consisting of 2 pcs., made of steel, painted black, weight: 2,1kg

- Sealing profile, pluggable or commercial sealing material on PU-basis