- Drainage channel with comb profile BG-FILCOTEN parkline NW 150 H 35 made of FILCOTEN HPC (high-performance concrete)

load-class A15 – C250 kN type M, according to EN1433 – CE-certified,

Channel element with integrated anchoring pockets, channel joint sealable,

Slot-width 12,5 mm, height 35 mm

Building biology tested and recommended by IBR (Institut für Baubiologie Rosenheim, DE)

Fire-behaviour class: A1 according to EN13501 - non-combustible

100% recyclable with U-A marking

Delivery and installation according to the manufacturer's installation instructions.

NW/Height:		LxWxH: [mm]	weight: [kg]	Capacity: [l/m]	eco-indicator: [kg]

NW150 H 35:	1000x150x35	9,2		1,1		CO2-Eq. 2,6

- Drainage channel with outlet, channel-element as described in position 1, but

with bottom outlet, connection for DN100 pipe socket

NW/Height:		LxWxH: [mm]	weight: [kg]	Capacity: [l/m]	eco-indicator: [kg]

NW150 H 35:	1000x150x35	8,9		1,1		CO2-Eq. 2,5

- cross-corner-element, made of FILCOTEN HPC

to build crossings, T-pieces and 90°-corners

NW150 H 35:	LxWxH: 150x150x35 mm		weight: 1,34 kg

- outlet cover, double bar, made of stainless steel 1.4301

for safe covering of the drain opening

NW150 H 35:	LxWxH: 108x68x60 mm		weight: 0,1 kg

- front cap closed, made of stainless steel 1.4301

NW150 H 35:	LxWxH: 1x138x24 mm		weight: 0,1 kg

- Installation chair, Kit incl. screws for positioning the channel, galvanised steel

weight: 0,6 kg

- Construction-time barrier, made of galvanised steel

NW150 H 35:	LxWxH: 1000x150x14 mm	weight: 1,5 kg

- Cleaning-rake, made of stainless steel 1.4301

NW150 H 35:	LxWxH: 89x123x68 mm		weight: 0,3 kg