- Drainage channel with comb profile BG-FILCOTEN parkline NW 150 H 50 made of FILCOTEN HPC (high-performance concrete)

load-class A15 – C250 kN type M, according to EN1433 – CE-certified,

Channel element with integrated anchoring pockets, channel joint sealable,

Slot-width 17 mm, height 50 mm

Building biology tested and recommended by IBR (Institut für Baubiologie Rosenheim, DE)

Fire-behaviour class: A1 according to EN13501 - non-combustible

100% recyclable with U-A marking

Delivery and installation according to the manufacturer's installation instructions.

NW/Height:		LxWxH: [mm]	weight: [kg]	Capacity: [l/m]	eco-indicator: [kg]

NW150 H 50:	1000x150x50	11,9		2,0		CO2-Eq. 3,3

- Drainage channel with outlet, channel-element as described in position 1, but

with bottom outlet, connection for DN100 pipe socket

NW/Height:		LxWxH: [mm]	weight: [kg]	Capacity: [l/m]	eco-indicator: [kg]

NW150 H 50:	1000x150x50	11,6		2,0		CO2-Eq. 3,2

- cross-corner-element, made of FILCOTEN HPC

to build crossings, T-pieces and 90°-corners

NW150 H 50:	LxWxH: 150x150x50 mm		weight: 1,8 kg

- outlet cover, made of stainless steel 1.4301

for safe covering of the drain opening

NW150 H 50:	LxWxH: 108x24x60 mm		weight: 0,1 kg

- front cap closed, made of stainless steel 1.4301

NW150 H 50:	LxWxH: 1x140x40 mm		weight: 0,1 kg

- Installation chair, Kit incl. screws for positioning the channel, galvanised steel

weight: 0,6 kg

- Construction-time barrier, made of galvanised steel

NW150 H 50:	LxWxH: 1000x150x14 mm	weight: 1,3 kg

- Cleaning-rake, made of stainless steel 1.4301

NW150 H 50:	LxWxH: 98x118x84 mm		weight: 0,2 kg