- Heavy-duty drainage-channel BG-CLASSIC BGZ-S NW 150 made of concrete,

with integrated Z-shaped cast iron edge,

load-class A15 – F900 kN, according to EN1433 – CE-certified,

channel joint with safety seam, sealable,

length 1000 mm, without or with 0,5 % slope,

Fire-behaviour class: A1 according to EN13501 - non-combustible

100% recyclable with U-A marking,

Delivery and installation according to the manufacturer's installation instructions.

NW/No.:		LxWxH: [mm]		weight: [kg]

150 No. 0:		1000x248x240		86

150 No. 5-0:		1000x248x265		91

150 No. 10-0:		1000x248x290		96

150 No. 20-0:		1000x248x340		105

150 No. 1-10:		1000x248x245-290	87 - 95

- Heavy-duty drainage-channel as described in position 1,

but overall length 500 mm, without slope

NW/No.:		LxWxH: [mm]		weight: [kg]

150 No. 0:		500x248x240		43

- Heavy-duty drainage-channel as described in position 1, but

with bottom outlet DN 150 (Dm 186 mm), for drainage-channels without slope

NW/No.:		LxWxH: [mm]		weight: [kg]

150 No. 0:		1000x248x185		82

150 No. 5-0:		1000x248x210		86,8

150 No. 10-0:		1000x248x235		91,5

150 No. 20-0:		1000x248x285		101

- Covers/Grates made of galvanised steel or ductile iron

with integrated longitudinal movement protection and quick-locking system (SV),

load class D 400kN – E 600kN, according to EN1433 - CE-certified

BG-CLASSIC SV mesh grating NW 150, galvanised steel

cl. D400, MW 30/10, length 1000 mm,

with integrated longitudinal movement protection and quick-locking system (SV), according to EN1433 – CE- certified

BG-CLASSIC SV mesh grating NW 150, galvanised steel

cl. D400, MW 30/10, length 500 mm,

with integrated longitudinal movement protection and quick-locking system (SV), according to EN1433 – CE- certified

BG-CLASSIC SV ductile iron slotted grating NW 150, cast iron EN-GJS

cl. D400, SW 18/170, length 500 mm

with integrated longitudinal movement protection and quick-locking system (SV), according to EN1433 – CE- certified

BG-CLASSIC SV ductile iron longitudinal bar grating NW 150, cast iron EN-GJS

cl. E600, MW 27/13, length 500 mm

with integrated longitudinal movement protection and quick-locking system (SV), according to EN1433 – CE- certified

- Covers/Grates made of cast iron inclusive bolting material 4-times

with integrated longitudinal movement protection,

load class E600kN – F900kN, according to EN1433 – CE- certified

BG-CLASSIC ductile iron longitudinal bar grating NW 150, cast iron EN-GJS

cl. E600, MW 27/13, length 500 mm

with integrated longitudinal movement protection, inclusive bolting material 4-times, according to EN1433 – CE- certified

BG-CLASSIC ductile iron slotted grating NW 150, cast iron EN-GJS

cl. F900, SW 15/75, length 500 mm

with integrated longitudinal movement protection, inclusive bolting material 4- times, according to EN1433 – CE- certified

Optional accessories cover:

SET- bolting material for mesh grating

steel, galvanised – consisting of 1 Stk. screw and 1 Stk. Mutter

SET- bolting material for cast grating

steel, black galvanised – consisting of 1 Stk. screw and 1 Stk. Mutter

- sump unit BG-CLASSIC BGZ-S NW 150 concrete with integrated cast iron frame

procedure: RDS DN 150

length 500 mm / width 261 mm / height 690 mm

Delivery and installation according to the manufacturer's installation instructions.

weight:	95 kg

- silt bucket to sump unit, plastic

weight: 0,7 kg

- drain trap made of PVC duct bends DN 150/87°, plastic

weight: 3,9 kg

- forsheda-sealing for bottom outlet DN 150, Elastomer

weight: 0,5 kg

- front cap closed off galvanized steel

weight: 0,6 kg

- end cap with outlet DN 150 off galvanized steel

weight: 0,7 kg