- prefabricated side-strip slabs LEFIX with attachment concrete and a concrete quality of at least C30/37 XC3/XD3/XF4/XA1 (increased frost and de-icing salt resistance)

Complete surface of the slab with a gradient to the outside of at least 3 percent

Groove-like tread structure, transverse to the direction of travel, for generation of:

- a rumble or warning effect when passing over

- a controlled, even drainage of the roadway

Tapered end faces for inner and outer radii

Toothing with tongue and groove for a non-displacing composite effect

Integrated spacers to prevent chipping during transport, storage and installation

The side-strip slabs must be laid in accordance with the manufacturer's installation instructions.

Type: 		LxWxH: [mm] 		Weight: kg] 	Installation radius: [m] 	Colour of attachment:

1000/500: 		1000x500x140/125 	149 		> 12 			grey / red

- prefabricated side-strip slabs LEFIX as described in pos. 1, but,

with length 450 mm and laying radius 6 m

Type: 		LxWxH: [mm] 		Weight: [kg] 	Installation radius: [m] 	Colour of attachment:

450/500: 		450x500x140/125 	65 		> 6 			grey / red

- prefabricated side-strip slabs LEFIX as described in pos. 1, but,

with length 250 mm and laying radius 6 m

Type: 		LxWxH: [mm] 		Weight: [kg] 	Installation radius: [m] 	Colour of attachment:

250/500:		250x500x140/125	36		> 4			grey / red

- prefabricated side-strip slabs LEFIX as described in pos. 1, but,

with opening for reflector post, length 1000 mm, colour grey

Type: 		LxWxH: [mm] 		Weight: [kg] 	Installation radius: [m] 	Colour of attachment:

1000/500 LPF:	1000x500x140/125	145		> 12			grey

- prefabricated side-strip slabs LEFIX as described in pos. 1, but,

with width 350 mm, length 1000 mm

Type: 		LxWxH: [mm] 		Weight: [kg] 	Installation radius: [m] 	Colour of attachment: 1000/350:		1000x350x140/130	107		> 16			grey / red

- additional charge reflection area, 1 pc. groove profile per side-strip slab

Colour: red or white

- lifting clamp, max. load 250 kg, weight 15 kg, opening width 55 - 535mm, for purchase or rental